ILLINOIS TOLLWAY                                                                                                 AC-230

CHECKLIST FOR

STRUCTURAL STEEL BOLTING

This checklist has been prepared to provide the field inspector a summary of easy-to-read step-by-step requirements relative to the proper installation of Structural Steel Bolting.  The following questions are based on information found in Tollway Supplemental Specifications, Tollway Standards, IDOT Standard Specifications, IDOT Highway Standards, IDOT Constructions Manual and current policy memorandums and letters.

The installation of fasteners in bridge connections is a critical element in the proper behavior of the structure.  All connections are to be installed, tightened and inspected in accordance with the latest issue of the critical connections as issued by the Research Council on Structural Connections of the Engineering Foundation.

1.	PRE-INSTALLATION INSPECTION

Have you read Section 505 of the Standard Specifications, the Supplemental Specifications, the Special Provisions and Section 500 of the Construction Manual?	____

Are all fasteners being stored in their original containers so that they are protected from dirt and moisture or intermixing of lots?  Lids should be on and the containers not stored under plastic.	____

Do all delivered fastener assemblies have approved manufacturer's markings?  Markings should be on the containers, not just the lids.  (505.04)(f)(3)f.1.	____

CONTAINER INFORMATION REQUIREMENTS:

- Manufacturer identification

- Contents

- Component lot numbers (verify with MCTR)

- R-C lot number

Have you received the required certifications from the mill, the manufacturer and/or distributor?  (505.04)(f)(3)f.2.	____

MILL TEST REPORT (MTR)  505.04(f)(3)e.1.

- From steel producer on their form

- One report for each component

- Report must contain following:

  - Heat number

  - Chemical analysis

  - Location where melted and manufactured

  - Location where tests conducted

  - Date of tests

MANUFACTURER CERTIFIED TEST REPORT (MCTR) 505.04(f)(3)e.2.

- From each component manufacturer to document any tests they performed

- Report must contain the following:

  - Mill heat numbers (verify with MTR)

  - Manufacturer lot number (verify with container)

  - Test results

| BOLT | A. | Proof load test minimum values: |  |  |  |  |  |  | 1/2 in. bolt | 12,050 lbs. |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  | 5/8 in. bolt | 19,200 lbs. |  |
|  |  |  |  |  |  |  |  |  | 3/4 in. bolt | 28,400 lbs. |  |
|  |  |  |  |  |  |  |  |  | 7/8 in. bolt | 39,250 lbs. |  |
|  |  |  |  |  |  |  |  |  | 1 in. bolt | 51,500 lbs. |  |
|  | B. | Wedge tensile test |  |  | (10o with no head failures ¼ in. to 1 in.) |  |  |  |  |  |  |
|  |  |  |  |  | (6o with no head failures over 1 in.) |  |  |  |  |  |  |
|  |  | minimum values: |  |  |  |  |  | ½ in. bolt |  | 17,050 lbs. |  |
|  |  |  |  |  |  |  |  | 5/8 in. bolt |  | 27,100 lbs. |  |
|  |  |  |  |  |  |  |  | ¾ in. bolt |  | 40,100 lbs. |  |
|  |  |  |  |  |  |  |  | 7/8 in. bolt |  | 55,450 lbs. |  |
|  |  |  |  |  |  |  |  | 1 in. bolt |  | 72,700 lbs. |  |
|  | C. | Hardness test |  | ≤ to 1 in. bolt |  |  | min. 24RC |  |  |  | max. 34RC |
|  |  |  |  | > 1 in. bolt |  |  | min. 19RC |  |  |  | max. 31RC |
|  | D. | Galvanization thickness |  |  |  |  | min. 2 ml. |  |  |  | max. 6 ml. |
|  | E. | R-C test |  |  |  |  |  |  |  |  |  |
|  |  | 1. Component lot number |  |  |  |  |  |  |  |  |  |
|  |  | 2. R-C lot number |  |  |  |  |  |  |  |  |  |
|  |  | 3. Location and date of tests |  |  |  |  |  |  |  |  |  |
| NUT | A. | Proof load test minimum values: |  |  |  |  |  |  | ½ in. nut |  | 20,450 lbs. |
|  |  |  |  |  |  |  |  |  | 5/8 in. nut |  | 32,550 lbs. |
|  |  |  |  |  |  |  |  |  | ¾ in. nut |  | 48,100 lbs. |
|  |  |  |  |  |  |  |  |  | 7/8 in. nut |  | 66,550 lbs. |
|  |  |  |  |  |  |  |  |  | 1 in. nut |  | 87,250 lbs. |
|  | B. | Hardness test |  |  |  |  | C and C3 nuts |  |  |  | B78 to C38 |
|  |  |  |  |  |  |  | DH and 2H nuts |  |  |  | C24 to C38 |
|  | C. | Galvanization thickness |  |  |  |  | min. 2 ml. |  |  |  | max. 6 ml. |
| WASHER | A. | Hardness test |  |  |  | black and mech. galv. |  |  |  |  | C38 to C45 |
|  |  |  |  |  |  | hot dip galv. |  |  |  |  | C26 to C45 |
|  | B. | Galvanization test |  |  |  |  |  | min. 2 ml. |  |  | max. 6 ml. |

4.	Certification statement

DISTRIBUTOR CERTIFIED TEST REPORT (DCTR)  505.04(f)(3)(e)(3)

- Prepared by distributor

- Documents R-C tests they performed and lot numbers assigned

- Must contain the following:

  - Manufacturer lot numbers (verify with MCTR)

  - R-C test results

  - Location and date of tests

  - R-C lot numbers

  - Certification statement

NOTE:  Galvanized fastener assemblies must have all physical tests performed after galvanization.  Therefore the test results could be on either the MCTR or the DCTR depending on who had the components coated.

Do all containers have an ILL OK stamp on them? If not, have you sent the required samples to Materials for testing?  No installation should begin until you have received the results.	____

Do all delivered fasteners have lubrication? Black fasteners should be oily to the touch; galvanized nuts should have a visible tinted lubricant on them. (505.04)(f)(3)(g)(2a & b), 1006.08	____

Have you the Contractor supplied a tension calibrating device?  The device must have been calibrated within the last year and the calibration results must be included.  The device must be capable of testing the following minimum bolt lengths  (505.04)(f)(2):	5/8” and 3/4” : 2”

7/8” : 2.25”

1” : 2.5”	____

Have you performed rotational capacity tests on two assemblies from each rotational capacity lot and recorded the results? (505.04)(f)(3)(g)(1)	____

# INSPECTION DURING INSTALLATION

Have you the Contractor demonstrated that the procedure to be used by the bolting crew will provide the required tension in a tension calibrating device?  Does each bolting crew member fully understand the tightening procedure to be used?  (505.04)(f)(2)	____

Are only enough fasteners that can be used during a work shift being removed from storage and are all unused fasteners being returned to storage in their original containers at the end of each work shift?	____

Are all of the holes in the splices and field connections being filled with bolts before any bolt tightening is begun?  On continuous span beams no bolt tightening shall begin until the entire length is in place. (505.04)(f)(2)	____

Are all fasteners in a connection being brought to snug tight before final tightening is begun? Snug tight should bring all the plies of a connection into contact with each other.  Start at the most rigid part (near the center) of the connection and work toward the free edges. (505.04)(f)(2)	____

Are all fasteners being brought to the required minimum tension in accordance with the Specifications?  Start at the most rigid part (near the center) of a connection and work toward the free edges. (505.04)(f)(2)	____

If at any time during installation you suspect the level of lubrication of the fastener has changed, are you conducting additional rotational capacity testing?	____

Are you monitoring the installation to assure that the installation method is being properly applied?	____

Are you inspecting each completed connection as required by the specification for the type of fastener used?	____

Galvanized and A490 bolts can not be reused.  A325 black bolts may be reused if allowed by your supervisor.  Additional tightening is not considered reuse.	____

TURN-OF-THE-NUT METHOD

After snug tightening has each bolt or socket been marked so that the required turn can be verified? (505.04)(f)(2)(d)	____

Is the unturned element being prevented from turning?	____

If impact wrenches are being used, are they of sufficient capacity so that the required turn is being performed in approximately 10 seconds?	____

Is tightening progressing from the most rigid part (near the center) to the free edges? 	____

Are all bolts being tightened using the required turn of the nut?	____

Are you visually checking the match marks to ensure that each fastener has been turned the amount necessary to achieve the required minimum tension?  (505.04)(f)(2)(d)(2)	____

TWIST-OFF BOLTS

Following the snug tightening operation, are all fasteners being tightened until the control or indicator element is twisted off?  (505.04)(f)(2)(b)	____

Is tightening progressing from the most rigid part (near the center) to the free edges?  (505.04)(f)(2)	____

Are you monitoring the tightening operation to ensure that the proper procedure is routinely being followed?	____

Are you visually checking that each control or indicator element has sheared?	____

Are you tapping each fastener with a hammer to ensure there are no loose fasteners?	____

Are you the Contractor cleaning and painting the exposed end?  Cleaning may be accomplished with a wire brush or power tool.  Painting shall consist of one coat (5.0 mils minimum thickness) of an approved high-build aluminum epoxy mastic. (505.04)(f)(2)	____

# LOCK PIN AND COLLAR

Following the snug tightening operation, are all fasteners being tightened until the control or indicator element is broken off? (505.04)(f)(2)(c)	____

Is tightening progressing from the most rigid part (near the center) to the free edges? (505.04)(f)(2)	____

Are you monitoring the tightening operation to ensure that the proper procedure is routinely being followed?	____

Are you visually checking that each control or indicator element has broken?  Are you randomly measuring the collar dimensions to ensure they are within the allowable tolerances shown in the manufacturer's table? (505.04)(f)(2)(c)	____

Are you the Contractor cleaning and painting the exposed end?  Cleaning may be accomplished with a wire brush or power tool.  Painting shall consist of one coat (5.0 mils minimum thickness) of an approved high-build aluminum epoxy mastic. (505.04)(f)(2)	____

DIRECT TENSION INDICATORS

Following the snug tightening operation, are you checking that the number of spaces in which a 0.005 inch gage is refused does not exceed the allowable value?  (505.04)(f)(2)(a)(2)	____

Is tightening progressing from the most rigid part (near the center) to the free edges?  (505.04)(f)(2)	____

Are you monitoring the tightening operation to ensure that the proper procedure is routinely being followed?	____

Are you visually checking that all gaps are not completely closed? (505.04)(f)(2)(a)(2)	____

Are you checking that the number of spaces in which a 0.005 inch gage is refused is equal to or greater than the allowable value?  (505.04)(f)(2)(a)(2)	____