ILLINOIS TOLLWAY									AC-190

CHECKLIST FOR
HOT- MIX ASPHALT (HMA) SHOULDERS

This checklist has been prepared to provide the field inspector a summary of easy-to-read step-by-step requirements relative to the proper construction of Hot-Mix Asphalt Shoulders (Section 482). The following questions are based on information found in Tollway Supplemental Specifications, Tollway Standards, IDOT Standards Specifications, IDOT Highway Standards, IDOT Construction Manual and current policy memorandums and letters.

Have you checked the contract Special Provisions, Supplemental Specifications and plans to see if any modifications have been made to the requirements listed herein?	____

# GENERAL

The work shall consist of constructing a HMA shoulder on a prepared subgrade, existing paved shoulder, or subbase.	____

HMA shoulders shall not be placed on frozen or muddy subgrade.	____

For pavement and shoulder resurface projects, HMA binder and surface course mixtures the same as that specified for the mainline pavement may be used in lieu of HMA shoulder mixture for the resurfacing of shoulders at the option of the contractor.	____

Shoulder strips 12 in shall be constructed of the HMA binder and surface course mixtures as that specified for the mainline pavement.	____

# 2.	SHOULDER GRADES

a.	Calculate and mark on the pavement edge, for both tangent and superelevated areas, the subgrade cut and offset for the shoulder structure shown on the plans.	____

b.	Prior to bituminous placement, the earth subgrade should be checked with an instrument or hand template to ensure the required depth and cross section of the completed shoulder will be obtained.  Refer to THICKNESS TESTS.	____

# 3.	SUBGRADE

The subgrade shall be prepared according to Section 301 or applicable special provision.	____

The subgrade shall be compacted to not less than 95% of the standard dry density and have a minimum IBV of 8.0.  The in place density of the completed shoulder subgrade will be tested every 1500 feet (Sampling Schedule I, CQP Specification).	____

When HMA shoulders are constructed adjacent to a pavement constructed on an improved (lime-modified) subgrade and additional material is needed to extend the improved subgrade to the bottom of the HMA shoulder, the additional material shall be subbase granular material, Type C, conforming to Section 311 (Art. 482.04).	____

The subgrade shall be drained during the placing and compacting of the bituminous shoulder by cutting lateral ditches through any adjacent berms of earth.	____

# 4.	PLANT AND MATERIALS

HMA Mixtures will meet the following requirements:

a.	Materials will meet the requirements of Section 1030 and applicable special provisions.	____

b.	Hot-Mix Plant will meet the requirements of Article 1102.01.	____	____

c.	The HMA shall be delivered at a temperature of 250 to 350 F (Art. 312.05)

# 5.	EQUIPMENT REQUIREMENTS

a.	The transportation of the HMA mixture shall conform to Article 1030.08.	_____

b.	Spreading and finishing machine. (Art. 312.04)	_____

c.	Tandem rollers shall be 6 to 12 tons total weight; 190 to 400 pounds per inch of width on drive wheel(s). (Art. 312.04)	____

d.	Self-propelled pneumatic-tired roller; not less than 300 pounds per inch of width of tire tread in contact with the HMA surface, tire pressure, 60 to 120 psi. (Art. 312.04)	____

e.	Vibrating rollers shall meet the requirements of Article1101.01(g).	____

f.	Trench roller, 300 to 400 pounds per inch of width on the compaction wheel. (Art. 312.04)	____

# 6.	TEMPERATURE RECORDS

Occasional temperature checks shall be taken and recorded from the delivered material in the truck and behind the spreading machine.	____

# 7.	PLACING AND COMPACTING

The bottom lifts shall be placed with a mechanical spreader approved by the Engineer.  The machine shall be operated from the mainline pavement.
(Art. 482.05)	____

When the shoulder width is 10 ft or greater, the top lift shall be placed with a spreading and finishing machine. (Art. 482.05)	____

The HMA mixture shall be spread to provide a minimum compacted lift in accordance with the table below.  A maximum compacted lift of 6 in is allowed provided the required density is obtained.  (Art. 312.05)	____

| Nominal Maximum Aggregate Size of Mixture | Minimum Compacted Lift Thickness |
| --- | --- |
| CA 12 – ½ in | 1 ½ in |
| CA 10 – ¾ in | 2 ¼ in |
| CA 6 – 1 in | 3 in |

The top lift shall be a maximum 3 in compacted layer.  (Art. 482.05)	____

Each layer shall be compacted using a vibratory compactor and a tandem roller.	____

On resurfacing projects with shoulder width of 6 ft or less, the shoulder resurfacing may be placed simultaneously with the traffic lane.	____

Shoulder resurfacing with widths greater than 6 ft shall be placed in a separate operation.	____

# 8.	DENSITY REQUIREMENTS

The HMA shoulder shall be compacted to meet the following density requirements
(Art. 1030.05 (3) (4)):

a.	The first layer shall be compacted to not less than 92% of the theoretical density.	____

b.	Subsequent layers shall be compacted to 93% to 97.4% of the theoretical density.	____

- The density of each layer will be obtained by approved nuclear methods or from specimens furnished by the contractor.

d.	Density testing frequency is one test per 1/2 mile per lift, per side, randomly located.  (Sampling Schedule 4, CQP Specification).	____

# 9.	THICKNESS TEST (Art. 482.06)

The thickness of the bituminous shoulder will be checked at least every 
1000 ft when the shoulder is constructed and paid for as a square yard unit of measure.

a.	Before and after cross sections with a rod and level, or before and after measurements taken from an established reference elevation such as a stringline or edge of pavement.	____

b.	Shoulder areas less than 90% of the plan nominal thickness shall be brought to the proper thickness by placing additional shoulder material or by complete removal and replacement of the deficient shoulder area.	____

c.	If corrective action is needed, the final shoulder elevation shall not exceed the plan elevation or elevation established by the engineer by more than 1/8 in.	____

# 10.	RUMBLE STRIPS (Section 642)

a.	Rumble strip pattern will be as shown on the plans.	____

b.	Corrugations shall be omitted when falling within the limits of a structure, or ramp entrance and exit.	____

c.	Equipment shall be a self-propelled milling machine with a rotary-type cutting head(s).	____